## Slide 1
CO adsorption on Pd(111) model
Updates
Simplified System

## Slide 2
450 K
Estimated values
k1_est = 7896.02
k2_est1 = 0.04948
k2_est2 = 0.06958
P = 0.001 Pa

## Slide 3
460 K
Estimated values
k1_est = 6690.8
k2_est1 = 0.10324
k2_est2 = 0.72797

## Slide 4
475 K
Estimated values
k1_est = 9314.7
k2_est1 = 0.1379
k2_est2 = 0.7935

## Slide 5
500 K
Estimated values
k1_est = 10018
k2_est1 = 0.1958
k2_est2 = 1.4068

## Slide 6
All fittings together

## Slide 7
Ea = 4.3409 kcal
A = 8.2688 * 105
Adsorption region

## Slide 8
Ea1 = 9.2812 kcal
A1 = 2.32 * 103
Ea2 = 25.83 kcal
A2 = 3.45 * 1011
Two desorption regions
Ea = 35.5 kcal/mol
A = 1* 1013.5
Guo, Xingcai, and John T. Yates Jr. "Dependence of effective desorption kinetic parameters on surface coverage and adsorption temperature: CO on Pd (111)." The Journal of Chemical Physics 90.11 (1989): 6761-6766.
Literature:

## Slide 9
Predicted vs Fitted
k1_est = 7896.02
k2_est1 = 0.04948
k2_est2 = 0.06958
k1_est = 6445.7
k2_est1 = 0.0721
k2_est2 = 0.0980
Predicted (from Arrhenius)
Estimated

## Slide 10
Predicted vs Fitted
k1_est = 6690.8
k2_est1 = 0.0851
k2_est2 = 0.1300
k1_pred = 8423.4
k2_pred1 = 0.0733
k2_pred2 = 0.1761
Predicted (from Arrhenius)
Estimated

## Slide 11
Ea = 2.1408 kcal
A = 8.7617 * 104
Adsorption region (-460K)
P = 0.001 Pa

## Slide 12
Ea1 = 12.4217 kcal
A1 = 5.8442 * 104
Ea2 = 27.14 kcal
A2 = 1.39* 1012
Two desorption regions (-460K)
Ea = 35.5 kcal/mol
A = 1* 1013.5
Guo, Xingcai, and John T. Yates Jr. "Dependence of effective desorption kinetic parameters on surface coverage and adsorption temperature: CO on Pd (111)." The Journal of Chemical Physics 90.11 (1989): 6761-6766.
Literature: