## Slide 1: All plots and summaries

## Slide 2: OUR DATA

## Slide 3: Frequency (time) – our data

## Slide 4: Mathematical Area (time) – our data
Smoothed with 5 moving average points
As is - No smoothing.
Note: I am not including the Absolute area since it is almost the same as the Mathematical.
Note: This is not updated for 470, 475 and 480.

## Slide 5: GERMAN PAPER DATA

## Slide 6: Digitized
Interpolated
Pressure of interest
We obtain expected coverage at saturation for each temperature.

## Slide 7: COVERAGE vs WAVENUMBER

## Slide 8: Constant pressure experiment (our data)
COV vs WV results
Chart: Coverage vs wavenumber
| 1.30388850284448E-2 | 2.9151625058612799E-2 | 5.8573857826438203E-2 | 8.09919269641656E-2 | 9.4303114530899596E-2 | 0.121633928218339 | 0.18187832257116801 | 0.24072561282194599 | 0.29752780932042999 | 0.31924873876469501 | 0.409326644407911 | 0.41921653701224199 | 0.45080193662469098 | 0.478862091758046 | 0.50552344796027304
Hoffman paper (300K) | 1822.818 | 1822.9304 | 1822.9588 | 1823.1741 | 1823.3805 | 1825.1489 | 1825.0136 | 1825.5545 | 1835.7707 | 1836.5659 | 1906.9112 | 1921.0498 | 1931.6287 | 1938.3333 | 1945.4236
Isotherm + Interpolated (450K) | 1820 | 1830.1547 | 1834.0117 | 1861.0108 | 1872.5819 | 1891.8669 | 1897.6525 | 1913.0805
Isotherm + Interpolated (475K) | 1814.73 | 1820.51 | 1820.51 | 1839.8 | 1843.65 | 1874.51 | 1882.22
Isotherm + Interpolated (490K) | 1820.51 | 1820.51 | 1839.8 | 1843.65 | 1874.51 | 1882.22
Chart: Pressure
| 1E-8 | 4.9999999999999998E-8 | 9.9999999999999995E-8 | 4.9999999999999998E-7 | 9.9999999999999995E-7 | 5.0000000000000004E-6 | 1.0000000000000001E-5
450K | 1820 | 1830.1547 | 1834.0117 | 1861.0108 | 1872.5819 | 1891.8669 | 1897.6525
475K | 1814.73 | 1820.51 | 1820.51 | 1839.8 | 1843.65 | 1874.51 | 1882.22
490K | 1812.8 | 1818.58 | 1820.5 | 1824.37 | 1834 | 1855.23 | 1864.87
our WV (P) data + COV (P) from slide 6 (German paper)

## Slide 9: Area normalized (testing)
i – refers to temperature Ti
ref – temperature chosen as reference
SAT – at saturation
Ai - area for temperature Ti
Normalized area

## Slide 10: Area - normalized
450 K as reference
490 K as reference

## Slide 11: Area - normalized
450 K as reference
490 K as reference

## Slide 12: Area - normalized
450 K as reference
490 K as reference

## Slide 13: - EXTINCTION COEFFICIENT

## Slide 14
Beer’s Law
Assuming we have the correct A, we can obtain at saturation and at 1/3.
@ SATURATION: green frame
we take mean of area points
we have at SAT from German paper
@ 1/3: blue frame
we take mean of area points
we have at 1/3 from (wv) conversion (using plot in slide 8)
Note: we believe that is constant below 1/3 ML, but it varies between 1/3 and SAT.